DESCRIPTION

TITAN HARDWALL is especially formulated for use as a hard veneer off white plaster finish on cement or gypsum plaster renders, plaster sheet board or cement fiber board. The same bag of plaster can be used in a plaster sand or a plaster perlite render.

TITAN OBH IS DESIGNED TO BE USED ON CEMENT SAND RENDER WITH ONLY PLASTIFLO PLASTISIZER IN THE RENDER MIX.

LIME PUTTY OR HYDRATED LIME POWDER IS NOT REQUIRED OR RECOMMENDED TO BE MIXED WITH TITAN OBH.

MIXING

Add 11-11.5 litres of clean, uncontaminated water to a squat drum, shake 20kg bag of TITAN into the water. Allow to soak through. Mix it thoroughly with a high shear propeller in an electric drill at speeds of 500-1000rpm. Mix to a creamy consistency which should take in the region of 3-5 minutes.

APPLICATION TO CEMENT RENDER

Most situations, the TITAN wet mix can be applied to the render without pre-damping. Brush the cement rendered walls with a soft hair broom to remove the loose unbound sand/cement on the surface of the render. Wet walls if required, only if suction is too high or if the daily temperature is very high. Apply the wet mix with a steel trowel. Lay it down flat and tight to the render coat leaving no trowel marks. Fill and dub with the TITAN OBH mix as trowelling the wet mix onto the render. It is usual to apply a scratch coat immediately followed by a full even coat to produce a flat even plane surface.

FINAL TROWELLING: The TITAN OBH coat on the wall is left flat and level until it firms and the set commence. This is about two (2) hours from time from making the mix. Finger pressure observation applied on the TITAN OBH setting mix on the wall determines when to final trowel. Also, a light brown colouration occurs over the wall indicating the plaster is setting. Use water on the trowel to give slide. It also eliminates any tearing of the finish.  Trowel until the surface is smooth and flat which is usually 2 to 3 skim trowel finish. The finished set plaster will have an eggshell to flat finish.

Remove mix from frames, power points and floors.

APPLICATION TO CONCRETE CEILINGS

Apply SCREEDBOND onto the ceiling as a liberal even coat. Trowel on dubbing mix as a filling coat onto bonding coat while bonding coat is wet, leveling while troweling on mix. Skim a finishing coat of TITAN OBH immediately over the laid dubbing mix. Final trowel and finish are done similarly as to when applying TITAN OBH to cement render.

APPLICATION TO FRESH RENDER-1 HOUR OLD

After ruling and finish trowel of the sand/cement render, e.g. 1 vol cement: 7 vols sand or less sand with the recommended addition of PLASTiFLO to the in-place render, it is able to be set plastered with TITAN OBH.

PROCEDURE FOR TITAN OBH APPLIED TO FRESH RENDER ONE HOUR OLD

Mix the TITAN OBH as previously described to produce a workable wet mix. Trowel on a scratch coat and follow with a full troweled coat, leveling off

and flattening as applying it.

Level off the TITAN OBH plaster applied to the fresh render and allow the plaster to come to near setting. Brown patches and finger pressing determines this period of time.

Finish trowel to a smooth flat plane finish which is closed in and firm.  Leave to allow TITAN OBH to fully set as a mat hard finish ready to accept paint (water-based paint is preferred).

COVERAGE

Coverage of a 20kg bag when mixed is approximately 16-17m2 on cement render.

CLEAN UP

All products mentioned are waterborne and can be removed with water while wet.

STORAGE

Store all products under cover, in a cool area, away from foodstuffs, in a sealed airtight container when not in use. Avoid contact with moisture

SAFETY

Wear coverall, safety boots and glasses. Gloves are optional to wear but highly recommended.

PACK SIZES

TITAN is sold in packs of 20kgs.

TRANSPORT

TITAN is not a hazardous good as defined by Safe Work Australia.

NOTE: PLASTIFLO is a product manufactured and sold by CALMARC CHEMICALS.