DESCRIPTION

DOUBLE R combines a unique blend of ingredients which have the property of retarding cement mixes in a consistent time. DOUBLE R is suitable to be used as a retarder for exposed aggregate concrete.

DIRECTIONS

General cement/sand screeds addition rate is from 1-2% by weight on the content of cement in the mix. Addition rate is calculated on the time of retardation required.

For exposed aggregate apply DOUBLE R to have an application onto the wet concrete. Before the initial set so the application is 2% of the estimated cement content in the layer of cement aggregate removed the following 24 hours to create exposed aggregate concrete.

CLEAN UP

Clean any spills with water.

SAFETY

Keep out of reach of children. Do not swallow.  Avoid contact with eyes. Wash hands after use. Do not mix with other cleaning products. Dispose of empty containers with household rubbish.

FRIST AID

For advice, contact a doctor or poisons information centre. Phone Australia 131126. If swallowed, do NOT induce vomiting. Give a glass of water to drink. If skin or hair contacts occurs, remove contaminated clothing and flush skin and hair with running water. If in eyes, hold eyelids apart and flush the eye continuously with running water. Continue flushing until advised to stop by the Poisons Information Centre or a doctor or at least 15 minutes.

STORAGE

Store all products under cover, in a cool area, away from foodstuffs, with lids on when not in use.

PACK SIZES

DOUBLE R is sold in packs of 5 and 20 litres.

TRANSPORT

DOUBLE R is a non-hazardous good as defined by Safe Work Australia.